## Slide 1
1A. Savoy Navarro
1R. Sefri
1J. F.Genat*
1J. David
1M. Dhellot
1 E. Hornero
*currently on leave of absence at U. Chicago
1J. F. Huppert
1A. Charpy
2A. Comerma
3Denis Fourgeron
3Richard Hermel
LPNHE, Universite Pierre et Marie Curie/IN2P3-CNRS
University of Barcelona/Electronics Department
LAPP/IN2P3-CNRS
Avec la contribution de:
Ecole Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
ECOLE MICROELECTRONIQUE
CIRCUIT de FRONT-END POUR DETECTEUR A MICRO-PISTES DE SILICIUM EN TECHNOLOGIE CMOS 130nm
Thanh Hung PHAM

## Slide 2
Ecole Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
Outline
Front-end chip pour silicon strips detector at the ILC
A 4-channel chip in 130nm CMOS
A 88-channel mixed mode chip in 130nm CMOS
Perspective & Conclusion

## Slide 3: The ASIC is designed to work at:
Ecole Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
Silicon strips readout at the ILC
The ILC machine cycle imposes the running condition of the detectors/electronics
Long shaping time (slow machine)
Power cycling (possible)
Digitization and pre-processing :
Take advantage of time between inter-bunch trains
200 ms

## Slide 4
Ecole Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
A 4-channel chip in CMOS 130nm
Waveform
Counter
12-bit single ramp ADC
Ch #
Analog memory(6MHz)
iVi > th
Sparsifier
Channel n+1
Channel n-1
Preamp +
Shaper
reset
Clock 48 MHz
reset
Trigger
Synopsys of 4-channel chip
3mm
130nm chip layout et photo
1.5mm

## Slide 5
A 4-channel chip in CMOS 130nm
Ecole Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
Synopsys of analog pipeline
SHIFT REGISTER 16 bits
WRITE
READ
RESET
INPUT
OUTPUT
CLK
START
Gnd
T1
T2

## Slide 6
A 4-channel chip in CMOS 130nm
Ecole de Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
Offset ramp
Analogue Input
Ramp Input
Offset ramp
Slope ramp
Buffer ramp
Startconv
G
R
A
Y
C
O
U
N
T
E
R
Latch
Clk_48MHz
M
U
L
T
I
P
L
E
X
E
R
LH
12b
8b
RST
Synopsys of single ramp ADC

## Slide 7
A 4-channel chip in CMOS 130nm
Ecole de Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
ENC@0.8ms = 733.7 + 14.63 electrons/pF
ENC@2ms = 613 + 9 electrons/pF
Preamplifier & Pulse shape simulation

## Slide 8
Input
DC sampling
Positive input of inv-adder
Shaper output
Adder-inverter output
Sparsifier output
tdelay
Time (ns)
Simulation of sparsifier (1/2)

## Slide 9
A 4-channel chip in CMOS 130nm
Ecole de Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
Analog pipeline
9
No of sample | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16
Voltage difference(mV) | 33 | 4.83 | -1.1 | -2.3 | -2.3 | -2.4 | -2.6 | -2.5 | -2.4 | -2.6 | -2.6 | -2.6 | -2.5 | -2.5 | -2.5 | 0.2
Input ramp of pipeline
Ramp reconstructed with analog pipeline
Time (ms)
V(mV)
-300
-400
-500
-600
10
11
12
Analog pipeline simulation

## Slide 10
A 4-channel chip in CMOS 130nm
Ecole Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
10
DNLmax = 7LSB
DNLrms = 1.36LSB
INLmax = 7LSB
INLrms = 2.74LSB
ADC Measurements

## Slide 11
Input = 50mV
Sampling rate = 6MHz
Calibration capacitance = 256fF
Non uniformity of gain due to non-uniformity of calibration capacitor
A 4-channel chip in CMOS 130nm
Ecole Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
Analog pipeline measurement

## Slide 12: Measurement with sensor Response to Sr90
A 4-channel chip in CMOS 130nm
Ecole Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
HPK sensor
Average S/N about 15 (2x9.15cm=18.3 cm strip length)

## Slide 13
A 88-channel chip in CMOS 130nm
Ecole Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
i-1
i+1
i
0
7
0
7
Preamplifier + CR-RC Shaper
Sparsifier
Bias generator:
Bias voltage (10bits), bias current (8bits), reference voltage (10bits)‏
refi
8x8 analog memories
Latch
Ramp
ADC
ADC REGISTER,
GRAY COUNTER
MULTIPLEXER &
OUTPUT INTERFACE
Input interface, Initial Setup
Main control : pipeline, time stamp, event stamp, calibration, A/D conversion
Calibration
inputi
Channel#i
Synopsys of 88-channel chip

## Slide 14
Layout and silicon die of a 88-channel chip
5mm
10mm
Analogue
Bias control
Digital
Layout
Picture of the silicon die
Bonding diagram of the packaged chip
A 88-channel chip in CMOS 130nm
Ecole Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM

## Slide 15
98x10-bit registers
Serial input(48Mhz clock)
Analog bias (DAC)
Channel threshold simulation
(Mixed-mode simulation)
A 88-channel chip in CMOS 130nm
Ecole Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
Initialization & Input Interface

## Slide 16
A 88-channel chip in CMOS 130nm
Ecole
Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
Write state

## Slide 17
SiTR_130-88 + FPGA in metalic box
Oscilloscope
Logic analyzer
PC and C++ based program allows the control of the circuit
USB link
A 88-channel chip in CMOS 130nm
Ecole Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
Lab test bench

## Slide 18
Linearity of the preamplifier and the shaper
Measured power dissipation per ch (wrt all the analog chain up and including the ADC):
~1.35mW/channel
Measured gain ~ 43mV/MIP
@ 2.6% of nonlinearity up to 24MIP
A 88-channel chip in CMOS 130nm
Ecole Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
Test of the analogue part

## Slide 19
Conclusion & Perspective
Ecole Microélectronique, 11-16 oct 2009, La Londe les Maures, Thanh Hung PHAM
A first front-end chip has been designed and tested that allows to validate the choice of technology and architecture.
A second front-end chip with 88 channel was not fully tested but introduce us to a complex circuit.
A new 128-channel chip is under development with an optimization in silicon surface by using 2f Mimcaps capacitor .
Direct connection to detector is under investigated